Last data updates: 29 March 2013

Ho, Y.S. and Wang, C.C. (2008), Sorption equilibrium of mercury onto ground-up tree fern. Journal of Hazardous Materials, 156 (1-3), 398-404.

| Document type: Article | Language: English | Cited references: 56 | Times cited: 12 | Times self cited: 0 |
| --- | --- | --- | --- | --- |

Abstract: The sorption behavior of mercury at different temperatures onto ground-up tree fern was investigated. The experimental results were fitted to two two-parameter isotherms, the Freundlich and Langmuir isotherms, as well as to two three-parameter isotherms, the Redlich-Peterson and Sips isotherms to obtain the characteristic parameters of each model. A comparison of best-fitting was performed using the coefficient of determination and Chi-square test. Both the Langmuir and Redlich-Peterson isotherms were found to well represent the measured sorption data. According to the evaluation using the Langmuir equation, the saturated monolayer sorption capacity of mercury ions onto ground-up tree fern was 26.5 mg/g at 298 K. It was noted that an increase in temperature resulted in a higher mercury ion loading per unit weight of the tree fern. In addition, various thermodynamic parameters, such as ΔG degrees, ΔH degrees, and ΔS degrees, were calculated and compared with the sorption of mercury by other sorbents. (C) 2008 Elsevier B.V. All rights reserved.

Author Keywords: Agriculture Product; Adsorption; Mercury; Tree Fern; Biosorption

KeyWords Plus: Industry Waste-Water; Aqueous-Solutions; Metal-Ions; Adsorption-Isotherms; Activated Carbons; Bagasse Pith; Coconut Husk; Hg(II) Ions; Basic Dye; Removal

Reprint Address: Ho, YS (reprint author), I Shou Univ, Dept Chem Engn, 1, Sect 1, Hsueh Cheng Rd, Ta Hsu Hsiang, Kaohsiung Cty 840 Taiwan

Addresses:

1. I Shou Univ, Dept Chem Engn, Ta Hsu Hsiang, Kaohsiung Cty 840 Taiwan

E-mail Addresses: ysho@isu.edu.tw

- Rivas, J., Toral, M.I. and Richter, P. (2012), Sorption of polybrominated diphenyl ethers in biosolid model samples. Journal of the Chilean Chemical Society, 57 (2), 1087-1090.

- Wang, X.M., Deng, R.J., Jin, X.Y. and Huang, J.H. (2012), Gallic acid modified hyper-cross-linked resin and its adsorption equilibria and kinetics toward salicylic acid from aqueous solution. Chemical Engineering Journal, 191, 195-201.

- Ma, N.F., Chen, S.X., Li, T.Y. and Zhang, Q.K. (2012), Removal of mercury by an aminated fiber prepared by irradiation grafting copolymerization. Separation Science and Technology, 47 (6), 867-874.

- Sun, C.M., Ma, F., Zhang, G.H., Qu, R.J. and Zhang, Y. (2011), Removal of mercury ions from ethanol solution using silica gel functionalized with amino-terminated dendrimer-like polyamidoamine polymers: Kinetics and equilibrium studies. Journal of Chemical and Engineering Data, 56 (12), 4407-4415.

- Gong, R., Du, Y., Li, C., Zhu, S., Qiu, Y. and Jiang, J. (2011), Thioglycolic acid esterified into rice straw for removing lead from aqueous solution. Iranian Journal of Environmental Health Science & Engineering, 8 (3), 219-226.

- Kaghazchi, T. and ShamsiJazeyi, H. (2011), Modification of activated carbon using a NOx-containing gaseous by-product for enhanced Hg(II) removal from aqueous phase. Journal of Industrial and Engineering Chemistry, 17 (3), 608-614.

- Lu, L.C., Wang, C.I. and Sye, W.F. (2011), Applications of chitosan beads and porous crab shell powder for the removal of 17 organochlorine pesticides (OCPs) in water solution. Carbohydrate Polymers, 83 (4), 1984-1989.

- Alagumuthu, G., Veeraputhiran, V. and Venkataraman, R. (2011), Fluoride sorption using Cynodon dactylon-based activated carbon. Hemijska Industrija, 65 (1), 23-35.

- Gong, R.M., Cai, W.K., Li, N., Chen, J.A., Liang, J.J. and Cao, J.X. (2010), Preparation and application of thiol wheat straw as sorbent for removing mercury ion from aqueous solution. Desalination and Water Treatment, 21 (1-3), 274-279.

- Ma, F., Qu, R.J., Sun, C.M., Wang, C.H., Ji, C.N., Zhang, Y. and Yin, P. (2009), Adsorption behaviors of Hg(II) on chitosan functionalized by amino-terminated hyperbranched polyamidoamine polymers. Journal of Hazardous Materials, 172 (2-3), 792-801.

- Basha, S., Murthy, Z.V.P. and Jha, B. (2009), Sorption of Hg(II) onto Carica papaya: Experimental studies and design of batch sorber. Chemical Engineering Journal, 147 (2-3), 226-234.