## Slide 1
Conclusions
The design model presented is based on a pseudo-second-order kinetic model, and this has been used for minimizing the reaction time used in a two-stage contact system that operating cost would be reduced.
The model has been optimized with respect to contact in order to minimize total contact time to achieve a fixed percentage of cadmium ions removal using a fixed mass of tree fern.
Two-Stage Batch Adsorber Design Using Pseudo-second-order Kinetic Model for the Adsorption of Cadmium Ions onto Tree Fern
Ming-Huang Wang1#, Pei-Yu Lin1, I-Hsin Lin1, Yu-Ting Feng1 and Yuh-Shan Ho2
1School of Public Health, Taipei Medical University
2Bibliometric Centre, Taipei Medical University - Wan-Fang Hospital
Introduction
The cost and performance of product/equipment/system or the mode of application are always of concern to control the process efficiency. Therefore the adsorption capacity and required contact time are two of the most important parameters to understand in an adsorption process. It is important to determine how adsorption rates depend on the concentrations of adsorbate in solution and how rates are affected by adsorption capacity or by the character of adsorbent in terms of kinetics. From the kinetics analysis, the solute uptake rate which determines the residence time required for completion of the adsorption reaction may be analysed and established. This approach has been adopted and is presented in the present paper.
Materials and Methods
All contact investigations were carried out using a baffled, agitated 2 dm3 adsorber vessel. Samples (2 ml) were withdrawn at suitable time intervals, filtered through a 0.45 m membrane filter and then analysed cadmium ion concentration. A fixed mass of tree fern was added to each 1.7 dm3 volume of cadmium solution and a constant agitation speed was used for all experiments.
Batch Adsorber Design
STAGE 1
STAGE 2
S1
C0
q0
L
q0
S2
C1
L
q1
S1
q2
S2
C2
L
Figure 1. Schematic for two-stage countercurrent batch adsorption
Pseudo-second-order kinetic model
Mass balance equation
Figure 1: Comparison of 95% cadmium removal time of each stage in two-stage process
Table 1. Parameters for effect of initial concentration on the Cd(II)/tree fern system
Table 1. Minimum contact time for various percentage cadmium removal in a two-stage process