## Slide 1
The Kinetics of Sorption of Lead Ion onto Palm Kernel Fiber
Yu-Ting Feng1#, Ming-Huang Wang1, Wen-Ta Chiu2,3 and Yuh-Shan Ho4*
1School of Public Health, Taipei Medical University
2Graduate Institute of Injury Prevention and Control, Taipei Medical University
3Department of Neurosurgery, Taipei Medical University - Wan-Fang Hospital
4Bibliometric Centre, Taipei Medical University - Wan-Fang Hospital
Introduction
Equilibrium analysis is fundamental for the evaluation of the affinity or capacity of a sorbent. However, thermodynamic data can only predict the final state of a system from an initial non-equilibrium mode. It is, therefore, important to determine how sorption rates depend on the concentrations of sorbate in a solution and how rates are affected by the sorption capacity or by the character of the sorbent in terms of kinetics. In the present research, kinetic studies were carried out using an agitation batch sorber to study the effects of the initial solution pH and fiber dose. A kinetics analysis was carried out to correlate the experimental data based on a pseudo-second-order kinetics model. In addition, an isotherm was predicted by changing fiber doses using the equilibrium concentration and equilibrium capacity obtained based on the pseudo-second-order constants.
Results
Methods
A range of initial solution pH values (pH 3–6) was used, and flasks were agitated for 20 min. All contact investigations were performed in a 1-dm3 flask. A 0.6 g sample of palm kernel fiber was added to 400 ml of a lead ion solution and agitated at 200 rpm for all experiments. For the effect of sorbent dose, a range of palm kernel fiber doses from 1.5 to 5 g/dm3 was used, and agitation was carried out for 20 min. A reaction temperature of 36±3 °C was used for each 400 ml volume of lead ion solution with an initial concentration of 120 mg/dm3, and an agitation speed of 200 rpm was employed. The experiments were carried out at an initial lead concentration 120 mg/dm3 for all studies. Samples (2.5 ml) were withdrawn at suitable time intervals and filtered, and the filtrate was analyzed for the remaining lead concentration with atomic absorption spectrophotometry (AAS).
Table 2. Isotherms and their linear forms
Table 3: Pseudo-second-order rate parameters for sorption of lead on palm kernel fiber at various initial solution pH values
Table 1. Pseudo-second-order rate parameters for sorption of lead on palm kernel fiber at various palm kernel fiber doses
Conclusions
The pseudo-second-order rate constant, the initial sorption rate, and the equilibrium sorption capacity were a function of palm kernel fiber dose. An isotherm was obtained by changing fiber doses using the equilibrium concentration and the equilibrium capacity obtained based on the pseudo-second-order constants. It is not appropriate to use the coefficient of determination of the linear regression analysis to compare the best fit of the Freundlich and both linear Langmuir isotherms. Non-linear Chi-square analysis may be a better method. Freundlich is a special case of the Redlich–Peterson isotherm, when constants A and B are high. It was clear that both the two-parameter pseudo-Freundlich and the three-parameter pseudo-Redlich–Peterson isotherms were the best-fitting models for the experiment results.
Figure 1. Variation in the sorption capacity and percent lead removal against the fiber dose.
Figure 2. Pseudo-isotherms of the sorption of lead on palm kernel fiber with operating lines.